TAJIMA DOORS

SECTION 08430

BRONZE CLAD DOORS AND ENTRANCES

## PART I – GENERAL

  - DESCRIPTION:

- Work includes interior and exterior entrance doors and frames, sidelites

and transoms where applicable, thresholds and hardware as specified

in the drawings

- Related work not included:

- Lock cylinders

- Glass and glazing

- Sealants between frames and masonry.

- Structural members

  - SUBMITTALS:

### Shop drawings: Includes elevations and plans, detail sections in full or one-half size showing glass and metal thick nesses, typical joint details, field connections, anchorage, fasteners, door and frame reinforcements, material types and finishes.

### B.   Samples: Two 4” x 6” material sample indicating color and texture to be submitted

  - QUALITY ASSURANCE:

###### A.   The manufacturer must have been regularly engaged in the manufacture and installation of Bronze/Stainless Steel/Steel doors for a period of no less than ten (10) years.

B.   All doors and frames must be engineered and fabricated by

the same manufacturer

  - WARRANTY

###### All Tajima manufactured and installed entrance and framing systems shall be warranted against defective materials and workmanship for 5 years after completion of installation

- This warranty is not intended to cover adjustments made necessary by the         shifting or settling of the building structure.

#### PART II – PRODUCTS

  - ACCEPTABLE MANUFACTURER

- Tajima Door Division, Tajima Corp USA

  - MATERIALS AND ACCESSORIES

- Material:

Bronze Door: alloy # 464 Naval Brass

Finish:  #4  Satin, #8 Mirror or Non directional graining,

Medium or Dark Statuary Finish, Lacquered

Reinforcement: Stainless Steel 16 Gauge minimum

Frames: 11, 14 or 16 Gauge

- Fasteners:

Steel or Stainless steel anchors

- Stile and Rail profiles or seamless

face   as shown on drawings

Bottom rail height may be stipulated by

Code.

D.  Doors:

- Bronze door shall be formed from a minimum of .06” thick material.

- Formed bronze doors shall have .06” thick stainless steel reinforcement.

- Joint between stiles and rails shall be butt. Where  welding on joint is

necessary, surfaces will be grinded smooth.

- Finish is to be applied to the door after fabrication.

- Door thickness shall be 1 3/4” to 2”

- Top rail:  3-1/2” high or higher preferred; 2-3/4” minimum.

- Bottom rail:  6” minimum.

- All reinforcing material to be welded to door body.

E.  Frames:

- Bronze frames shall be formed from a minimum of .06” thick material

with minimum 16 gauge stainless steel reinforcement

- Minimum face dimension of frame to be 1 5/8”

- Minimum depth of frame to be  1/2”

- Consult factory for dimensions less than those above

- Frames shall be erected without  the use of exposed screws where feasible

- The finish is to be applied to the frame after fabrication to ensure a

blemish-free finish

F.  Weather strip:

- Shall be manufacturer’s standard polypropylene pile or as specified on the drawings

- Shall occur:

- Vertically at meeting stiles on pairs of doors.

- At Top and Bottom rails.

- At door stops at both hinge and strike jambs.

- Thresholds:

- Shall be furnished if specified

- Finish hardware:

- Hardware shall be as specified in Finish Hardware Section

2.3 FABRICATION:

- Fabricate components in accordance with approved shop drawings.  Shop fabricate to greatest extent practicable to minimize field cutting, splicing and fastening.  Remove burrs from cut edges.

- Fabricate system as indicated on approved shop drawings.  Any welding shall be in accordance with AWS standards, performed by qualified welders.  Do not distort members or deface exposed finish.  Grind exposed welds smooth.

- Factory preparation per manufacturer templates for finish hardware.  Mortise and reinforce frames and door stiles and rails to receive finish hardware in accordance with approved shop drawings

D.	Prior to leaving factory, all doors and frames shall be assembled and “hung”.    All necessary adjustments shall be made to provide proper perimeter clearance between door and frame and all coordination between door, frame and finish hardware shall be tested.

#### PART III – EXECUTION

# 3.1 Inspection

- Openings shall conform to details and dimensions shown on the approved shop drawings.

- The Contractor prior to installation must correct conditions that may adversely affect the door installation.

# 3.2 Installation

  - All materials shall be installed by factory-trained erectors in strict accordance

  - With installation data provided by factory and these specifications

  - All doors shall be adjusted after glazing contractor completes his work and

  - Install doors in strict accordance with the approved shop drawings and all local, state, and national laws and building codes.

  - Set doors plumb, level, and true to line, without warp or rack of frames.

  - Anchor door frames securely to surrounding construction with approved fasteners.

  - The exterior joints between the frames, trim and mullions shall be properly sealed watertight with an approved sealant and be neatly pointed.

  - Any abraded surface of the doors and frames finish shall be cleaned and touched up with air dry paint furnished by the door manufacturer, in a color to match the factory applied finish.

# 3.3 Cleaning

- The General Contractor shall be responsible for protecting the doors, frames and related materials during storage on the job and during and after installation.

- Installer shall leave the doors and frames surfaces clean after installation, exercising care to avoid damage to protective coatings and finishes.

- Any protection necessary due to the cleaning of materials adjacent to the doors and frames shall be the responsibility of the General Contractor.